Description of review design, scope, and methods

Review design and scope

This study is a scoping review of published research on the assessment of parchment damage (PDA). The objective was to map the analytical techniques used to assess parchment condition and damage, identify patterns of technique use and co-use, and examine how authors describe the impact of techniques using terms related to invasiveness and destructiveness. It was designed and reported in accordance with the PRISMA-ScR (Preferred Reporting Items for Systematic Reviews and Meta-Analyses extension for Scoping Reviews) checklist.

In this Article, parchment damage assessment (PDA) is defined as the structured evaluation of parchment condition using observable features and measurable markers that reflect physical, chemical, biological, or mechanical alteration of the collagen-based support. From a PDA perspective, damage includes both macroscopic manifestations (e.g., cockling, shrinkage, gelatinization, cracking, abrasion, discoloration, and losses) and underlying material changes that increase the risk of future failure even when the surface appears intact. Methods were considered PDA methods when they were used to detect, localize, classify, or quantify deterioration or vulnerability of the parchment substrate. Studies focused solely on inks, pigments, or text recovery were included only when they explicitly assessed impacts on the parchment substrate or reported substrate condition markers.

This scoping review maps published analytical and experimental PDA research and does not capture the full breadth of practice documented in treatment reports, institutional protocols, or practitioner knowledge.

## Eligibility criteria

### Inclusion criteria

- Population: Parchment artefacts, manuscripts, documents, or fragments (including both intact objects and detached fragments) from heritage contexts.

- Concept: Experimental or applied work that assessed parchment condition or damage (i.e., generated observational or analytical evidence about degradation, vulnerability, or damage state), including studies on historical parchments and newly manufactured / experimentally aged parchments. Both quantitative and qualitative assessments (including structured visual assessment) were eligible.

- Context: Studies and reports situated in cultural heritage conservation, archival science, and materials science, including work led by conservators, laboratories, or collaborations between them, provided that the paper included case material and reported assessment outputs.

- Source types and language: Peer-reviewed articles, technical reports, theses, and other gray literature (e.g., museum or professional society reports), and conference proceedings published in English or French.

### Exclusion criteria

- Guidance-only papers (e.g., general method guides, practice guidance, or overview documents) that did not report original assessment data (inputs/outputs) on parchment objects or samples. These documents may be valuable for practice, but they do not contribute primary evidence to the technique-frequency mapping and risk-inflating counts through conceptual duplication.

- Studies focused solely on leather or leather-based heritage materials without a parchment substrate.

- Studies focused solely on inks, pigments, artworks, or text recovery on parchment without assessing damage to the parchment substrate (e.g., pigment analysis only).

- Studies focused solely on dating (e.g., radiocarbon) or animal species identification (e.g., ZooMS/PMF) were excluded unless the work also reported substrate condition, degradation, or vulnerability markers relevant to parchment damage assessment

- Studies focused solely on palimpsest discovery/reading methods when they did not assess damage or condition of the parchment material.

- Papers that reviewed ethics of characterization/damage assessment without reporting original assessment data on parchment objects or samples.

Operational note. Several domains (e.g., species identification, dating, palimpsest detection) can appear within broader characterization studies; such papers were included only when they also reported outcomes relevant to parchment damage/condition assessment.

## Search strategy

### Databases and aggregators

We conducted a comprehensive search using Google Scholar, Web of Science, and Scopus, selected for its broad coverage of peer-reviewed literature and its indexing of grey literature and technical reports commonly used in conservation and heritage science. Search strings included English and French terms related to parchment damage assessment and characterization, including:

- “parchment damage” OR “parchment assessment” OR “parchment characterization” OR “parchment characterisation”

- “collagen degradation in parchment”

- “conservation of parchment” OR “parchment stabilization” OR “parchment stabilisation”

- “dégradation du parchemin” OR “caractérisation du parchemin” OR “conservation du parchemin”

- “glycation of collagen in parchment” OR “glycation du collagène sur parchemin”

To improve the breadth of our corpus capture, we performed citation tracking, reference list screening, and hand-searching of key journals in cultural heritage and archival science. We concluded this process in November 2024.

## Study selection and relevance screening

Records were screened in two stages (title/abstract, then full text). Studies were retained when they reported assessment evidence about parchment damage/condition (e.g., physical deformation markers, collagen chemical/structural markers, thermal stability markers, microstructural markers, or biological indicators) obtained from historical or experimental parchments.

## Data extraction and field mapping

For each included publication, we extracted bibliographic metadata (title, authors, year) and coded study attributes relevant to field mapping. We recorded parchment type as:

- Historical parchment: material originating from heritage collections and treated as culturally/historically significant (e.g., manuscripts, charters, fragments with documented provenance); or

- Experimental parchment: newly manufactured, commercially obtained, or laboratory-prepared parchment (including artificially aged samples).

Classification was based on explicit descriptions in the methods/materials; when ambiguous, we inferred category from contextual cues (e.g., stated provenance, collection references, or study aims).

We then catalogued all damage assessment techniques reported, preserving authors’ stated method labels (e.g., FTIR, DSC, light microscopy, Raman, XRF, SEM–EDS) and subsequently normalizing these into a controlled vocabulary for quantitative analysis. We also coded:

- whether the author team included conservation expertise, laboratory expertise, or both (conservator-led, laboratory-led, collaborative);

- the reported interaction framing where provided (e.g., non-destructive, destructive, invasive, non-invasive), recognizing that these terms are used inconsistently and are analyzed separately in the terminology section; and

- additional assessment dimensions where present (e.g., humidity sorption, microbial analysis).

This structured extraction enabled an organized overview of methodologies across the corpus and supported analysis of technique prevalence, co-use patterns, and gaps in reporting and adoption.

Data availability. Please contact the corresponding author for the data.

Synthesis of results

We used descriptive mapping and narrative synthesis:

- Frequency and coverage: tabulated counts of techniques across the corpus and by parchment type (historical vs experimental).

- Co-use patterns: cross-tabulations and co-occurrence matrices of techniques used together within the same study; where useful, co-use was visualized as network diagrams (technique nodes, co-use edges, weighted by frequency).

- Stratified summaries: breakdowns by team expertise (conservator-led, laboratory-led, collaborative), by interaction framing (e.g., non-destructive vs destructive), and by additional dimensions (e.g., humidity sorption, microbiology).

- Terminology analysis: qualitative synthesis of how interaction and risk terms were used (non-destructive, invasive, etc.), noting inconsistencies and linking usage to the underlying procedural details when reported.

Critical appraisal of individual sources of evidence

Because this is a scoping review, critical appraisal was conducted to contextualize findings rather than to exclude studies. We applied a structured descriptive appraisal focused on methodological transparency and risk of bias across heterogeneous study designs:

- Sampling and representativeness: clarity on object/sample selection, number of items, ageing/conditioning protocols (for experimental parchments), and relevance to PDA.

- Measurement and instrument reporting: description of instruments and settings (e.g., spectral ranges/resolution, calibration and standards), environmental controls (humidity/temperature/light), and repeatability/replicates.

- Construct validity for “damage/condition”: whether the measured markers are theoretically and empirically linked to parchment deterioration (e.g., collagen denaturation markers, shrinkage temperature, fiber morphology).

- Outcome reporting completeness: reporting of raw/summary data, uncertainty (e.g., SD/SE, confidence intervals), and data availability.

- Analytical bias and confounding: handling of known confounders (e.g., previous treatments, surface soiling, ink/pigment interference, hydration history), and whether blinding/randomization were applicable and used.

- Interaction and risk framing: clarity and evidence supporting labels such as “non-destructive,” “invasive,” or “destructive,” including sample removal, surface alteration risk, and mitigation strategies.